## Slide 1: Robustness of Steel Connections in Fire
Collaborative project: University of Sheffield + University of Manchester
Objective: Investigate the performance of joints in fire, especially their ability to act as ties to maintain structural integrity
Joint temperatures: Thermal testing and modelling of joints (Manchester)
Joint robustness: Common steel joints to be tested at elevated temperatures and rationalised via FE modelling (Sheffield)
Component models to be created for analysis of these connections in full-frame software
Subframe tests to be done towards the end to validate compnent models

## Slide 2: Test facility and test design
Furnace
Reaction frame
Loading Jack

## Slide 3: Test measurement
Reaction frame
Mirror
Camera 1
Camera 2
Strain gauges
Loads measured by strain gauges fixed to two loading bars
Deformations measured by cameras placed at the front and top of the furnace

## Slide 4: View of the test setup
Setup of the reaction frame and the furnace
Setup of the test specimen
View from camera 1

## Slide 5: Why special loading system?
Connection should be allowed to rotate at least 18° before fracture.
Movement of loading bar must stay within 300mm furnace hole
Length and position of the 3 load bars are selected to satisfy these requirements
Screw Jack moving downward
Φ300mm furnace hole
18o

## Slide 6: Calculation of the maximum load
Flexible Endplate
Fin Plate
Flush Endplate
Web Cleat
FE analysis used to estimate maximum joint resistance
Strongest - determines the strength of the load system

## Slide 7: Schematic of parametric study
20
550
650
750
0.7
1.0
1.4
Flexible endplate
Fin plate
Web cleat
Temperatures
Each plane is one connection geometry - tested for whole temperature range, various loads.
Vertical extension represents 1 to 3 special connection geometries - tested to observe different failure combinations.
Tension/shear force ratio
Flush endplate

## Slide 8: Preliminary bolt tests
Bright bolts (grade 8.8) specified to BS 4190
Black bolts (grade 8.8) specified to BS EN ISO 4014, nuts ordered to BS EN ISO 4032
Four types of combination
  Bright bolts with grade 10 nuts (GA), 7H/8g
  Black bolts with grade 10 nuts (GB), 6H/6g
  Bright bolts with grade 8 nuts (GC), 7H/8g
  Black bolts with grade 8 nuts (GD), 6H6g
Previous tests showed evidence of occasional thread stripping

## Slide 9: Failure modes of bolts
GB: black bolts with grade 10 nuts, 6H/6g
Tensile failure in the thread part of bolts

## Slide 10: Failure modes of bolts
GD: Black bolts with grade 8 nuts, 6H/6g
Threads of nuts stripped off

## Slide 11: Animation of bolt test

## Slide 12: Thermal Tests
Standard fire exposure
Four connection types to column major axis: fin plate, flexible end plate, flush end plate, web cleats. Connection to column minor axis: fin plate
Four fire protection (intumescent coating) schemes: no protection, column, column + beams, column + beams + bolts
Temperature measurements in beams, columns, connectors, shear studs, decking, reinforcement, concrete

## Slide 13: Thermal Analysis
Using ABAQUS
Calibrate Eurocode calculation procedure: method of calculating effective section factors
Optimise fire protection strategy

## Slide 14: Structural Fire Tests
Standard fire exposure, same connection types as in thermal tests, unprotected, composite beams
Columns to provide longitudinal restraint to beams: beams in bending and catenary action until connection fracture
Two beam loading levels (max. & min.), two column sizes (for beam bending only/for beam in catenary action)
Connection (fin plate/flush end plate) behaviour in cooling

## Slide 15: Structural Analysis
Using ABAQUS: solid and shell elements
Detailed variation of forces in connectors during heating and cooling
Comparison with VULCAN analyses: global behaviour of beams/columns + component based representation of connectors
Development of robust connection types

## Slide 16: Work to be continued
JOINT TESTS
Finish testing four types of joints.
64+ specimens
Put models into
global structural analysis program
SUB-FRAME TESTING
(University of Manchester)
Validation
SIMPLE MODELS
Adapt the T-stub model to endplate type joints
Develop models for fin plate joints
Develop models for web-cleat joints
Develop simplified thermal models
THERMAL TESTS
Temperature distributions for different joints & fires
FEM ANALYSIS
Simulate the test result
Study the failure mechanism
Provide theoretical bases for the simple model