## Slide 1: Connection design by Component Based Finite Element Method Lecture 2 Joint of hollow to open section

## Slide 2: List of lectures
Beam to column moment connection
Joint of hollow to open section
Column base
Seismically qualified joints

## Slide 3: Aims and objectives
Provide information on modelling of hollow section joints
Provide an online training to students and engineers
Introduce principles of Failure Mode model
Introduce principles of Component Based Finite Element Method (CBFEM)
Show the process of Validation & Verification
Offer list of references relevant to the topic

## Slide 4: Lecture 2 Joint of hollow to open section
František Wald, Marta Kuříková, Martin Kočka
Lubomír Šabatka, Jaromír Kabeláč, Drahoš Kojala

## Slide 5: Tutorial
This lecture describes principles of FEM modelling of hollow section joints by applying the Component Based FEM (CBFEM).
The failure mode models are presented on one of the most simple case on hollow to open section joints.
Survey of both simple and FEM analyses and modelling is shown.
Validation, Verification and Benchmark cases using Component based Finite Element Method are presented.
Material was prepared under the R&D project MERLION II supported by Technology Agency of the Czech Republic, project No TH02020301.

## Slide 6: Motivation
The aim of this lecture is to explain the design of hollow sections joints on joints of hollow sections to open sections, as a simple case of very large subject.

## Slide 7: Outline of the lecture
Introduction - hollow section joints
Failure mode method
  General
  Influencing joint parameters
  Component method
  Hollow to open joints
  Assessment I
Component based FE method
  Principles
  Validation
  Verification
  Benchmark case
  Assessment II
Summary

## Slide 8: Hollow section joints
Lecture 2
Joint of hollow to open section

## Slide 9: Geometry
The welded joints of circular, square or rectangular hollow sections can be either:
  Uni-planar
  Multi-planar
The combination of hollow sections with open sections are used in the uni-planar joints.

## Slide 10: Basic geometrical types
  The typical uni-planar joints
K joint
KT joint
N joint
T joint
X joint
Y joint

## Slide 11: Basic geometrical types
  The typical multi-planar joints
DK joint
X joint
DY joint
KK joint
TT joint
XX joint

## Slide 12: Loading
The design resistance of the joint is expressed as maximum axial or moment resistances for the brace.
The moment resistance can be reached for in-plane or out-of-plane loading.
Mip,Ed
Mop,Ed
NEd
Mip,Ed
NEd

## Slide 13: Design of welds
The welds are preferably designed for full resistance of joint not be the weakest part. I.e. the design resistance of the weld, per unit length of perimeter of a brace member, should not normally be less than the design resistance of the cross-section of that member per unit length of perimeter.
The full seam butt weld is recommended for ti > 8 mm with a = ti
The fillet welds are recommended only for members thickness ti  8 mm with the weld effective thickness a for element thickness ti and for steel
  S 235 as a = 0,92 ti
  S 275 as a = 0,96 ti
  S 355 as a = 1,10 ti
  S 420 as a = 1,42 ti
  S 460 as a = 1,48 ti

## Slide 14: Design methods
Design resistance of joints may be determined by:
Failure mode method based on
  Curve fitting procedures with derived joint parameters based on analytical models
Component method
  Using lever arms and component resistances determined according to a failure mode procedure
Finite element method

## Slide 15: Finite element method
  Research oriented model by numerical experiments with geometric and material non-linear analysis with imperfections and evaluation of safety as mechanical experiments according to EN1990.
  Design oriented model with geometric and material non-linear analysis using design material model.
      The Component based FEM (CBFEM) is design procedure combining analytical models for components and FE analysis of plates.

## Slide 16: Failure mode model
Lecture 2
Joint of hollow to open section

## Slide 17: Failure modes on chord demonstrated on rectangular hollow sections (RHS)
Chord face failure
Punching shear failure of the chord face
Overall shear failure of the chord
Chord side wall failure

## Slide 18: Failure modes on brace demonstrated on rectangular hollow sections (RHS)
Brace failure
Local buckling
of the brace member
Local buckling of the chord face

## Slide 19: Excluded modes of failure
Weld failure
  Excluded by use efficient throat thickness of the welds
Lamellar tearing
  Excluded by material properties
Local buckling of the chord or brace sections
  Excluded by using sections with can be classified to a maximum cross section class 2

## Slide 20: Design principle
Welds are designed for full sectional resistance.
Geometrical types are selected.
Range of validity is prepared based on available experiments for each geometrical type.
Limited number of failure modes is possible by each geometrical type.
For each geometrical type is prepared for each failure mode a curve fitting prediction of resistance.
The influencing joint parameters are derived based on five analytical models.

## Slide 21: Experiments and design resistance by curve fitting procedures
The design resistance is derived from experiments from
  Ultimate load (in EN1993-1-8:2005)
  Deformation limit (in prEN1993-1-8:2017)
    chord width as b0/300
Chart: Displacement, mm
Analytical model EN3-1-8:2005 | 23.35 | 23.35 | 23.35
Analytical model EN3-1-8:2020 | 9.34 | 9.34 | 9.34
Experiment
Model EN3-1-8:2006
Model EN3-1-8:2021
  Example behaviour and curve fitting predictions of joint with RHS chord 150 x 100 x 4 mm and brace 50 x 30 x 4 mm

## Slide 22: General limits of application
The members of lattice structures should satisfy the requirements:
Class 1 (or Class 2) cross section only
The angle between the brace and the chord should be larger than 30°
θ ≥ 30°

## Slide 23: Analytical Models for determination of influencing joint parameters
The curve fitting procedure is used for evaluation of joint´s resistance on each possible failure mode.
For the determination of the influencing joint parameters of welded joints between rectangular hollow sections are used analytical models:
  Yield line
  Punching shear
  Brace effective width
  Chord side wall bearing or buckling
  Chord shear

## Slide 24: Yield line model for the influencing joint parameters
The typical case of searching for influencing parameters by yield line model is chord face failure, as is shown below on deformed shape of K joint of RHS after experiment and its cut.

## Slide 25: Geometry of K shape joint of rectangular hollow section
li
κi
N1
g
h0
Θ1
Θ2
N2
d
d
b0
b1
α
In principle, the yield line model is an upper bound approach
Various yield line pattern have to be examined in order to obtain the lowest capacity
Strain hardening effects and membrane action not considered

## Slide 26: Limits of application of Yield line model
For joints with
small  ratios the deformations may be too high to realise the yield line pattern
medium  ratios the yield line model gives a good estimate of the chord face plastification capacity
high  ratios prediction of an infinite strength
where  is the ratio of the mean diameter or width of the brace members, to that of the chord. For T, Y and X joints it is d1/d0; d1/b0 or b1/b0. brace diameter/chord diameter; brace diameter/chord width or brace width/chord width

## Slide 27: Geometry of punching shear model for the influencing joint parameters
0,5·be,p
0,5·be,p
h1/sinΘ1
Very small gap
g = b0 – b2
Big gap
h2 / sinQ2
N1
h1
t0
1

## Slide 28: Punching shear model for the influencing joint parameters
Punching shear is caused by the brace load component perpendicular to the chord face.
Since of the non-uniform stress distribution at connection and not sufficient deformation capacity may be available, only parts of connection perimeters are effective for punching shear failure.
Therefore the punching shear criterion is

## Slide 29: Brace effective width model for the influencing joint parameters
N1
h1
0,5·beff
Q1
Similar to punching shear failure but the complete brace load has to be taken into account.
For a T, Y and X joint, the effective width criterion is
N1 = fy1 t1 (2h1+2be– 4t1)
As for punching shear failure the gaps are important for the effective lengths.

## Slide 30: Brace effective width model for the influencing joint parameters
For K-joints with gaps in the allowed range the brace effective width criterion is N2 = fy2 t2 (2h2+b2+be– 4t1)
No regulations for small gaps available
For big gaps the criterion for T-, Y- and X-joints can be used

## Slide 31: Chord side wall bearing/buckling model for the influencing joint parameters
T, Y and X joints with a high  ratio generally fail by yielding or buckling of the chord side walls.
For joints with  = 1,0 the yield capacity of the chord webs is determined as
N1
h1
t0
Q1
2,5·t0
2,5·t0
h1/sinQ1 +5t0
h0
b1
t1
b0
t0

## Slide 32: Chord side wall bearing/buckling model for the influencing joint parameters
For slender walls the yield stress fy0 is replaced by a buckling stress fk which is obtained from the European buckling curve a
For a Euler strut with a buckling length of h0 - 3t

## Slide 33: Chord shear model for the influencing joint parameters
Resistance is calculated based on the basic formulae for plastic design.
M
M
V
V
Ni,Rd
N0,gap
N0,gap
g
Q1
AV
h0
b0
t0

## Slide 34: Chord shear model for the influencing joint parameters
The plastic shear load capacity is
with an effective shear area AV = (2h0 + α ∙ b0) t0
Based on the Huber Hencky-Von Mises criterion the following interaction formula for shear resistance of the chord web
AV
h0
b0
t0

## Slide 35: Component based approach for hollow section joints
Lecture 2
Joint of hollow to open section

## Slide 36: Principle
Component based approach for hollow section design is formal reorganisation of equations to be engineering user friendly.
Failure modes are represented as components.
The same equations are used by curve fitting approach but in different formulation.
θ1
θ2
Brace 1
Brace 2
Chord
Joint 1
Joint 2
Joint configuration

## Slide 37: Defined lever arms and components (failure modes)
kfa factors transferred to
  beff effective widths
  ra lever arm
The interaction of load limits the application.

## Slide 38: 7 failure modes are modelled as 7 components
Chord face in bending
Chord side wall in tension/ compression
Chord side wall in in shear
Chord face under punching shear
Brace flange and web in tension/compression

## Slide 39: Application of principles to hollow to open joints
Lecture 2
Joint of hollow to open section

## Slide 40: Hollow to open joints as example of application
Types of joint available in failure mode method
  T, Y, X, K and K gap joint
Two failure modes only
  Brace failure
  Chord web failure
  Chord shear failure (only for K joint)
Range of validity
  Class 1 and 2 with limited flange width
Influencing parameters
  beff brace effective width
  bw chord web effective width
X joint
Y joint
K joint
T joint

## Slide 41: Design resistance of welded joints between RHS or CHS brace members and I or H section chords by failure mode method
Brace failure
Chord web failure
For K gap joints also chord web failure

## Slide 42: Design resistance of welded joints between RHS or CHS brace members and I or H section chords by failure mode method
Chord shear failure for K gap joints and for X joints with use

## Slide 43: Effective width of welded joints between RHS or CHS brace members and I or H section chords for failure mode method
For RHS braces

## Slide 44: Range of validity for welded joints between CHS or RHS brace members and I or H section chord members for failure mode method
Type of joint | Joint parameters |  |  |  |  | 
 | Chord web width dw | and or |  |  |  | Gap
 |  | Compression | Tension |  |  | 
X | Class 1 and | Class 1 or 2 and |  |  | Class 1 or 2 | 
T or Y | Class 1 or 2 and |  |  |  |  | 
K gap |  |  |  |  |  | 
Type of joint | Joint parameters |  |  |  |  | 
 | Chord web width dw |  |  |  |  | Gap
 |  | Compression | Tension |  |  | 
X |  |  |  |  | Class 1 or 2 | 
T or Y |  |  |  |  |  | 
K gap |  |  |  |  |  | 

## Slide 45: Component approach of welded joints between RHS or CHS brace members and I or H section chords by failure mode method
Brace failure from failure mode method

## Slide 46: Component approach of welded joints between RHS or CHS brace members and I or H section chords by failure mode method
Chord web failure from failure mode method
can be overwritten for component method as

## Slide 47: Assessment I
What limits the application of component method to hollow section joint design?
How are applied the analytically derived parameters in failure mode design procedure?
What failure modes are excluded and how?
Why are used range of validity?
Is the failure mode method the curve fitting one?
What is the principle of component method prepared based on failure mode method?
What failure modes may be observed at hollow to open section joints?

## Slide 48: Component Based Finite Element Method
Lecture 2
Joint of hollow to open section

## Slide 49: Material
Bilinear ideal elastic plastic diagram is used in design oriented models as CBFEM according to Ch. 7 in EN 1993-1-5:2006 and the slope of plastic branch is due to numerical stability E/1000.
Plastic strain in plates is limited by 5%.
In research oriented models is calculated the true stress-strain diagram from the material properties obtained in tensile tests, which is taking into account the necking of the coupon during its yielding before rupture.

## Slide 50: Plate and cross sections
For modelling of plate are applied four node quadrangle shell elements with six degrees of freedom. I.e. there are three translations and three rotations in every node.
The cross section is build from plates with independent meshes, which are connected by constraints, to simplify the meshing procedure.

## Slide 51: Welds
Wald et al. (2016)
t
σ
Weld throat section
Equivalent solid element
Equivalent stress
Multipoint constraint
Multipoint constraint
Filled weld is modelled by equivalent solid elastoplastic element, which is added between plates to express the weld behaviour, see Fig. below.
The element respects the weld throat thickness, position, and orientation to assure a good representation of weld deformation stiffness, resistance and deformation capacity.
The plastic strain in weld is limited to 5% as in basic material.

## Slide 52: Verification & Validation
The need and position of Verification & Validation in prediction of the reality is demonstrated on the diagram below
  ISO/FDIS 16730 Fire safety engineering - Assessment, verification and validation of calculation methods, Geneva, 2008.

## Slide 53: Design and research oriented model
Current approval of design models consist of
  Experiments
Research oriented FE model (ROFEM)
  Validated on experiments
  Numerical experiments
Design numerical model (DOFEM)
  Verified to numerical experiments and/or another design models
  Sensitivity study
  Validity range
Benchmark case (BC)
  To help the users of model to check up its correctness and proper use
Experiment
Research model
Design model

## Slide 54: Experiments with T joint of hollow to open section
In compression
In bending

## Slide 55: Experiments in compression
Geometry
Failure modes
A3 - Brace failure A1 - Chord web failure

## Slide 56: Results of experiments in compression

## Slide 57: Research oriented FEM
ABAQUS 6.13
Solid quadratic element (20-node brick, C3D20)
True stress-strain multilinear material model

## Slide 58: Boundary conditions for research oriented FEM
Bottom flange boundary condition
  Rotation and translation restrain in all axis
Load point
  Coupling to top of braces edges

## Slide 59: Validation of failure modes
Both failure modes were well predicted
Failure of chord web, experiment A1
Failure of brace, experiment A2

## Slide 60: Mesh sensitivity study
The Figure below shows the importance of the mesh size to the prediction of behaviour of joint

## Slide 61: Description of local and global behaviour
Development of plastic zones
The first yielding in the chord web
5% strain
Full plasticity at the peak load

## Slide 62: Quality of prediction of resistance
The validation should answer the quality of prediction on global behaviour namely in important points of design.
Table below shows the prediction of resistance by deformation of upper surface b0/300 (used by curve fitting models) and 5% of strain (used by numerical models) for experiment in compression A1 with failure of chord web.

## Slide 63: Verification of T-joint and K-joint CBFEM model to failure mode procedure
A uniplanar T-joint and K-joint of a rectangular hollow section brace to an open section chord.
The brace section is RHS 140x70x10.
The chord sections are IPE, IPN, HEA a HEB.
The brace is loaded in tension/compression or by in-plane bending moment.

## Slide 64: Verification of T-joint and K-joint in compression
The prediction by component based finite element method (CBFEM) is verified with the failure modes (FM) implemented in EN 1993-1-8:2005.
Three failure modes occur in joints of the welded rectangular hollow sections to the open sections, e.g. the local yielding of brace (brace failure), the chord web failure and the chord shear.
Chart: Resistance by FM [kN]
| 424.5 | 486.6 | 563.29999999999995 | 631.4 | 237 | 296 | 322 | 413 | 507 | 551.79999999999995 | 537.55999999999995 | 611 | 689.1 | 745.54 | 798.1 | 851.9
Chord web | 400 | 536 | 597 | 590 | 264.9 | 309 | 351 | 431 | 530 | 577 | 490 | 581 | 643 | 697 | 747 | 795
Brace failure | 719 | 770 | 820 | 859 | 867 | 871 | 867 | 852 | 871 | 875
Chord shear | 182.8 | 222.6 | 149.2 | 174.2 | 192.2 | 247.2 | 303.2 | 389.2
CBFEM=FM | 0 | 2000
CBFEM=1,1 FM | 0 | 2000
CBFEM=0,9 FM | 0 | 2000

## Slide 65: Verification of T-joint in bending
The prediction by component based finite element method (CBFEM) is verified with the failure modes (FM) implemented in EN 1993-1-8:2005.
Two failure modes occur in joints of the welded rectangular hollow sections to the open sections, e.g. the local yielding of brace (brace failure) and the chord web failure.
Chart: Resistance by FM [kNm]
| 17.13 | 20.34 | 11.4 | 14.1 | 15.4 | 19.2 | 20.91 | 16.8 | 18.899999999999999
Chord web | 19.06 | 22.65 | 12.735 | 14.475 | 16.88 | 19.25 | 21.475 | 15.32 | 18.52
Brace failure | 20.9 | 23.85 | 26 | 28.5 | 23.25 | 26.75
CBFEM=FM | 0 | 2000
CBFEM=1,1 FM | 0 | 2000
CBFEM=0,9 FM | 0 | 2000

## Slide 66: Benchmark case Uniplanar T-joint between RHS brace and I chord
Input
  Chord: IPE270, Steel S235
  Brace: RHS 140x70x10, Steel S235
  Weld: Throat thickness aw = 10 mm, Fillet weld around the brace
Output
  Design resistance in compression/tension Fc,Rd = 431 kN
  Collapse mode is full yielding of the chord web
Plastic strain [%]

## Slide 67: Assessment II
How is modelled the material for research and how for design models?
What elements are recommended for plates?
How are modelled welds?
What is expected to be the accurate solution in mesh sensitivity study?
How differs validation from verification?
What are two major purposes of benchmark cases in application of FEA analyses?

## Slide 68: Summary
Lecture 2
Joint of hollow to open section

## Slide 69: Summary
The hollow sections to open sections joints belongs to family of hollow section joints.
There are three failure modes
  Brace failure
  Chord web failure
  Chord web shear failure in case of gap
Shear failure of the chord
Chord web failure
Brace failure

## Slide 70: Summary
The curve fitting methods are used for evaluation of design resistances by each possible failure mode.
Range of validity limits application of expressions to experimentally approved solutions only.
Component based approach is for design of some rectangular hollow sections great simplification.
For design of circular hollow sections brings unpleasant complexity.
For complex joints generally loaded can not be used.

## Slide 71: Prediction of global and local behaviour
T joint of RHS brace and HEA chord
Chord HEA180
Brace RHS 180x100x8.8
Steel S355
Weld throat thickness 11 mm

## Slide 72: Global and local behaviour
Chart: Rotation [mrad]
| 0 | 0.9 | 1.8 | 2 | 2.5 | 4.4000000000000004 | 7.7 | 13.4 | 18.8 | 25.4
1 | 0 | 10 | 19 | 21 | 25 | 33 | 40 | 45 | 47 | 48.5
Elastic stage
M = 10 kNm
φ = 0,9 mrad
Sj = 10,7 MNm/rad

## Slide 73: Global and local behaviour
Chart: Rotation [mrad]
| 0 | 0.9 | 1.8 | 2 | 2.5 | 4.4000000000000004 | 7.7 | 13.4 | 18.8 | 25.4
1 | 0 | 10 | 19 | 21 | 25 | 33 | 40 | 45 | 47 | 48.5
Plastification of the upper flange of RHS brace
M = 19 kNm
φ = 1,8 mrad
Sj = 10,7 MNm/rad

## Slide 74: Global and local behaviour
Chart: Rotation [mrad]
| 0 | 0.9 | 1.8 | 2 | 2.5 | 4.4000000000000004 | 7.7 | 13.4 | 18.8 | 25.4
1 | 0 | 10 | 19 | 21 | 25 | 33 | 40 | 45 | 47 | 48.5
Initial plastification in the open section web
M = 21 kNm
φ = 2,0 mrad
Sj = 10,6 MNm/rad

## Slide 75: Global and local behaviour
Chart: Rotation [mrad]
| 0 | 0.9 | 1.8 | 2 | 2.5 | 4.4000000000000004 | 7.7 | 13.4 | 18.8 | 25.4
1 | 0 | 10 | 19 | 21 | 25 | 33 | 40 | 45 | 47 | 48.5
Initial plastification in the weld
M = 25 kNm
φ = 2,5 mrad
Sj = 10,0 MNm/rad

## Slide 76: Global and local behaviour
Chart: Rotation [mrad]
| 0 | 0.9 | 1.8 | 2 | 2.5 | 4.4000000000000004 | 7.7 | 13.4 | 18.8 | 25.4
1 | 0 | 10 | 19 | 21 | 25 | 33 | 40 | 45 | 47 | 48.5
Initial plastification in the open section flange
M = 33 kNm
φ = 4,4 mrad
Sj = 7,6 MNm/rad

## Slide 77: Global and local behaviour
Chart: Rotation [mrad]
| 0 | 0.9 | 1.8 | 2 | 2.5 | 4.4000000000000004 | 7.7 | 13.4 | 18.8 | 25.4
1 | 0 | 10 | 19 | 21 | 25 | 33 | 40 | 45 | 47 | 48.5
Initial plastification in the RHS brace roundings
M = 40 kNm
φ = 7,7 mrad
Sj = 5,3 MNm/rad

## Slide 78: Global and local behaviour
Chart: Rotation [mrad]
| 0 | 0.9 | 1.8 | 2 | 2.5 | 4.4000000000000004 | 7.7 | 13.4 | 18.8 | 25.4
1 | 0 | 10 | 19 | 21 | 25 | 33 | 40 | 45 | 47 | 48.5
Full plastification through the open section web
M = 47 kNm
φ = 18,8 mrad
Sj = 2,6 MNm/rad

## Slide 79: Global and local behaviour
Chart: Rotation [mrad]
| 0 | 0.9 | 1.8 | 2 | 2.5 | 4.4000000000000004 | 7.7 | 13.4 | 18.8 | 25.4
1 | 0 | 10 | 19 | 21 | 25 | 33 | 40 | 45 | 47 | 48.5
The open section web reaches plastic strain 5%
M = 48,5 kNm
φ = 25,4 mrad
Sj = 2,2 MNm/rad

## Slide 80: What is the major reason of using CBFEM for Hollow section joints?
The design resistance of generally loaded complex hollow section joints may be by failure mode method only estimated.
The example of design procedure by CBFEM is shown below.
3D model
Finite element analyses
Design check

## Slide 81: Design tips
The most economical and common way to connect hollow to open sections is by direct connection without any intersecting plates or gussets, this also gives the most efficient way for protection and maintenance.
The connections between hollow and open sections can be easily made, since the connecting members are provided with straight end cuts only.

## Slide 82: Design tips
Tips to optimize design
Select relatively stocky chord
Select relatively thin brace
b1/b0 as high as possible
t1/t0 as low as possible
b1
b0
t1
t0

## Slide 83: Design tips
Tips to optimize joint design
Consider virtues of gapped K-connections
Gapped joints are easier and cheaper to fabricate.
Overlapped joints have higher static and fatigue strength and produce stiffer truss (reduced truss deflections).

## Slide 84: Thank your for attention
URL: steel.fsv.cvut.cz
František Wald, Marta Kuříková, Martin Kočka
Luboš Šabatka, Jaromír Kabeláč, Drahoš Kojala

## Slide 85: Notes to users of the lecture
Subject Design of hollow section joints of steel structures.
Lecture duration 60 mins.
Keywords Civil Engineering, Structural design, Steel structure, Trusses, Truss girder, Joint, Hollow section joint, Hollow to open section joint, Component Method, Component based Finite Element Method, Eurocode.
Aspects to be discussed Curve fitting models of joints, Failure mode models of joints, FE models of joints, Failure modes, Component method principle, Application of analytical modelling
Further reading relevant documents in references and relevant European design standards, Eurocodes including National Annexes.
Preparation for tutorial exercise see examples in References.

## Slide 86: Sources
Batista P. N., Component based finite element model
of hollow to open section connection, Master theses,
Czech Technical University in Prague, 2017.
Jaspart J.P., Weynand K., Design of hollow section joints using the component method, Tubular Structures XV, 2015, 403-410.
Lu L.H., de Winkel G.D., Yu Y., Wardenier I., Deformation limit for the ultimate strength of hollow section joints, Tubular Structures VI, Balkema, Rotterdam, 1994, 341-347.
Wald F. et al, Benchmark cases for advanced design of structural steel connections, Česká technika ČVUT, 2016.
Wald, F.; Kočka, M. et al, To the advanced design models of hollow section joints, Stahlbau, Holzbau und Verbundbau, Stuttgart, 2017, 176-181Wardenier, J., Hollow section joints. Delft University Press, 1982, Delft.
Wardenier, J., Hollow section joints. Delft University Press, 1982, Delft.
Wardenier J. at al, Design Guide for Structural Hollow Sections in Mechanical Applications, CIDECT, Köln, 1995.
Wardenier, J., Packer, J.A., Vegte, G.J. van der, Zhao, X.-L., Hollow sections in structural applications, CIDECT, 2nd Edition, Bouwen met Staal, Delft, 2010.

## Slide 87: References CIDECT
http://www.cidect.org/design-guides.html
https://www.aisc.org/technical-resources/cidect-design-guides/
Dutta, D., Wardenier, J. Yeomans, N., Sakae, K. Bucak, Ö., Packer, J.A. 1998. Design guide for fabrication, assembly and erection of hollow section structures. CIDECT Construction with hollow steel sections. TÜV Verlag Köln.
Kurobane, Y., Packer, J.A., Wardenier, J., Yeomans, N., 2004. Design guide for structural hollow section column connections. CIDECT Construction with hollow steel sections. TÜV Verlag Köln.
Lu, L.H., de Winkel, G.D., Yu, Y. & Wardenier, J. 1993. Deformation limit for the ultimate strength of hollow section joints. In P. Grundy & A. Holgate & B. Wong (eds), Proc. intern. Symp. on Tubular Structures, Melbourne, 14-16 December 1994. Rotterdam: Balkema.
Packer, J.A., Wardenier, J., Kurobane, Y., Dutta, D., Yeomans, N. 1995. Design Guide for circular hollow sections (CHS) joints under predominantly static loading. CIDECT Construction with hollow steel sections. TÜV Verlag Köln.
Wardenier, J. 1982. Hollow section joints. Ph.D. Thesis. Delft University Press, The Netherlands.
Wardenier, J. 2002. Hollow Sections in Structural Applications. Bouwen met Staal, Zoetermeer, The Netherlands.

## Slide 88: CIDECT Materials
Publication
www.cidect.org/en/Publications
Design tolls
www.cidect.org/en/Software
Fire design
www.cidect.org/en/Software/tubeFire.php

## Slide 89: Standards
ANSI/AISC 360-10, Specification for Structural Steel Buildings, AISC, Chicago, 2010.
IIW XV-1439-13 ISO/FDIS 14346, Static Design Procedure for Welded Hollow-Section Joints – Recommendations, Brussels, 2012.
EN1993-1-8:2005, Eurocode 3, Design of steel structures, Part 1-8, Design of joints, CEN, Brussels, 2006.
prEN1993-1-8:2018, Eurocode 3, Design of steel structures, Part 1-8, Design of joints, CEN, Brussels, 2018.
EN 10210-1:2006, Hot finished structural hollow sections on non-alloy and fine grain steels, Part 1: Technical delivery conditions, CEN, Brussels, 2006.
EN 10210-2:2006, Hot finished structural hollow sections on non-alloy and fine grain steels, Part 2: Tolerances dimensions and sectional properties, CEN, Brussels, 2016.
EN 10219-1:2006, Cold formed structural hollow sections of non-alloy and fine grain steels, Part 1: Technical delivery conditions, Part 2: Tolerances, dimensions and sectional properties, CEN, Brussels, 2006.