| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| Title | CH | #### CHAPTER 6 The contents of this chapter, with few exceptions, fits also for bridges, masts towers and other structures. It is not restricted to connections subject to static loading. Change title to “Connections”. | E, A |  |  |
|  | UK | # General Comments This chapter relies heavily on Annex J for the performance of joints. As this annex has been rewritten, although not as yet published, it is assumed that there will be extensive modifications to the whole chapter to align with the new annex. The following comments have been prepared to highlight various topics which will need consideration during the redrafting. Effective length of welds – the purpose of using an effective length is that some welding techniques, particularly manual metal arc, do not produce welds that are full size and free of porosity at the start position. Guidance should therefore be given on the effective length to be used in a such situation. Clearly much, if not all, of this chapter is applicable to connections subject to dynamic load, particularly wind load, in addition to static loads. Loads causing potential fatigue could be resisted by connections deigned to this clause provided a fatigue check was carried out in accordance with Chapter 9. The heading is therefore incorrect, see also clause 6.1.1 (3) which emphasises this point. | A R |  |  |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 6.1.1 | FI | 6.1.1 Introduction I propose that in some place in the chapter 6 similar formula as in the part EC3 part 1.3 clause 6.4 is given to the calculation of the second order moment in the connections. As general there are no design rules for long slotted holes in the case when the applied force is acting perpendicular to the “directions” of the holes. | R R |  |  |
| 6.1.1 (2) | FR | - Introduction (2) I The value of Mb shall be taken as Mb = 1.50 for the resistance of bolts subject to tension. Mb = 1.25 in other cases (bolts subject to shear punching shear of the bolt head and of the nut) The value of Mb shall be taken as Mw = 1..25 for steel Fe 360 Mw = 1..30 for steel Fe 430 and Fe E 275 Mw = 1.35 for steels Fe 510 and Fe E355 (As concerns the symbols used for steel grades, refer to the comment to 3.2) | R |  |  |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
|  | CH | 6.1.1 (2) P 137 Simplify the number of partial safety factors m for the ultimate limit state design of connections to one simple value mc = 1.25. Exceptions to this value can be introduced in the concerned clauses. Give also the partial safety factor for serviceability limit state design ms = 1.1 In this clause. | A |  |  |
|  | UK | 6.1.1 (2) REVIEW the values of the factors in the NADs to obtain the best agreement between those used in each country. | A |  |  |
| 6.1.1 (3) | CH | 6.1.1 (3) p 137 Leave out. | R |  |  |
| 6.1.2 (1) | CH | 6.1.2 (1) p 137 Leave out. | R |  |  |
| 6.1.2 (2) | FR | - Applied forces and moments. (2) C It is not always necessary to allow for second order effects (case of non-sway frames, see 5.2.5), or for initial imperfections in members (see 5.2.4.2). | A |  |  |
| 6.1.2 (2) | CH | 6.1.2 (2) p 137 A remark upon the effect of over strength in the parent material should be made here. | A, M |  | See UK comment |
| 6.1.2 (2) | UK | 6.1.2 (2) EDIT this clause to make it more succinct by simply stating that the connections should be designed for all the forces and moments derived from the global analysis. This would then, by implication, include the forces included in the clause. | R |  | Necessary clarification. |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 6.1.3(1) | FR | - Resistance of connections (1) C Here ‘fasteners’ means bolts, rivets, pins and other similar components. The resistance of a connection does not depend exclusively on the resistance of the fasteners or of the welds : the other components of the connection also affect this resistance (gussets, splices, plates, webs and flanges of the sections within the connection, etc.) | A |  |  |
| 6.1.3(2) | CH | 6.1.3 (2) p 137 leave out. | R |  | Essential |
| 6.1.3(3) | FR CH | (3) A The plastic failure mechanism within a connection is not always single. The mechanism leading to the lowest resistance shall then be chosen. When this mechanism is evident (simple mechanism), experimental confirmation is no longer justified. (3) Leave out. | R R |  | Covered in Annex J. |
| 6.1.4(1) | CH NL | - Design assumptions (1)(d) C Explicitly, the behaviour of the material is assumed perfectly rigid-plastic and the design model mechanism shall be kinematically admissible. 6.1.4(1) This clause is based on a non-linear (plastic) distribution of the internal forces. Is it also possible to adopt a set of rules for a linear-elastic distribution? | E R |  | Terminology breakdown? Not so. |
| 6.1.4(2) | FR | (2)C When a doubt remains as to the choice of the path with the greatest stiffness, several paths shall be considered. | R |  | Obvious |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 6.1.4(3) | UK | 6.1.4(3) REVIEW the statement that ordinary accuracy of fit up need not be calculated which is agreed BECAUSE but this is in conflict with the strict interpretation of 6.1.2 | E |  |  |
| 6.2.(1) | SE | 6.2(1) May be a good advice but it is certainly not a principle, so please delete. | A |  |  |
| 6.2.(2) | FR | (2) C The presence of eccentricities at intersections introduces secondary forces into the connections and alters the distribution of internal forces and moments within the members. Structures made of hollow sections are an example where the effect of eccentricity may be disregarded to some extent (see Annex K). It should be noted that the absence of eccentricity at intersections does not prevent the requirement to allow for local eccentricity effects in the design of the connection itself. | A R R |  |  |
| 6.2.(3) | FR UK | (3) A This simplification is valid only in the case of a single setting out line parallel with the member axis. 6.2.(3) REVIEW this clause in line with clauses 5.8.3 which states that, subject to certain conditions, eccentricities in “angles” as web members” may be ignored and 6.5.2.3 which says that they must be taken account of (along with other effects) by the use of certain formula. The result of these conflicts is too complicated for the design engineer. | A~-M E,A-M |  | Or 2 lines in a wide leg. |
| 6.3 | SE | 6.3 It should be clarified that bolts in clearance holes cannot sustain reversed shear loads. Either preloading or locking devices helps. | R |  |  |
| 6.3.(1) | CH | 6.3 (1) p 139 This clause is in contradiction to the title of chapter 6. Compare the general comment to this chapter. | A |  | But fatigue is in Chpt 9. |
| 6.3.(2) 6.3.2 | CH UK | 6.3 (2) p.139 Leave out “. because it is subject to reversal of shear load.” PROVIDE clauses for fitted bolts or CLARIFY the position regarding their use. Give clarification and guidance covering the following: - Tolerance on the hole diameters - Bearing resistance - Assembly - Any limitations assumed on the presence of threads in the bearing areas and shear plane. - Presence of threads in bearing and shear planes. | R A |  |  |
| 6.3.(3) | FR D | (3) C In common buildings, displacements possibly due to some slip in this type of connections do not affect the efficiency of the bracing systems and may be disregarded in front of the global frame imperfections defined in 5.2.4.3. - Section 6.4 and 6.9 should be merged together, so that they are more condensed. A proposal is enclosed. - Classification of connections - General - The structural properties of all connections shall be such as to achieve the assumptions made in the analysis of the structure and in the design of the members. (2) Connections may be classified: - by rigidity, see 6.4.2 - by strength, see 6.4.3 | - A |  | Comment only – no action Part of re-write to include Annex J |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
|  | CH | - The types of connections should conform with table 5.2.1 depending on the member design assumptions and the method of global analysis, see 5.2.2. - The characteristics of a connection shall be consistent with the assumptions made in the global analysis of the structure and with the assumptions made in the design of the members, see 5.2.2.1. 6.4 p139 This paragraph can be shortened and simplified: e.g. - classification is not necessary, is a good help for students to explain the different types of connections, but has not to be repeated in a code - 6.4.1 is a repetition of 6.1.2 | R |  |  |
| 6.4.1 (2) | FR | (2) C The most commonly used connections have some deformability which may be characterised by a moment- rotation diagram M -  (see fig. 6.9.1) for the definition of the moment and of the rotation). For instance, figure a hereafter shows the moment-rotation relationship for four well known joint types. The behaviour is generally non-linear, but in order to make the elastic or plastic global analysis more simple, it may be necessary to identify a stiffness (linear behaviour) or a resistance level (as for a plastic hinge). Figure b shows, as a dotted line, an example of possible approximation to define those two values. | - |  | Comment only – no action |

| # Clause No | ## Country | ### Remarks and comments |  | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | Figure a | Figure b |  |  |  |
| 6.4.1 (3) | FR | (3) C In addition, the connections designed by means of the elastic theory should not be used in a structure analysed on the basis of the rigid-plastic theory, unless the elastic limit resistance of these connections is greater than the ultimate resistance of the members they connect. On the contrary, there is no incompatibility in using connections designed by means of the plastic theory if the structure is analysed on the basis of an elastic method (allowing for the stiffness of the connections if these are semi-rigid). |  | - |  | Comment only – no action |
| 6.4.2 | D | - Classification by rigidity. - Nominally pinned connections (1) A nominally pinned connection shall be so designed that it cannot develop significant moments which might adversely affect members of the structure. |  | A-M |  | Part of re-write |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 6.4.2 | D CH | - A connection may be classified as nominally pinned if its rotational stiffness S (based on a moment rotation characteristic representative of its actual anticipated behaviour) satisfies the criterion: S, < 0,5 EIb ___ Lb Where Sj is the initial rotational stiffness of the connection Ib is the second moment of area of the connected beam Lb is the length of the connected beam - 6.4.2 can be left out, if (1) is integrated in 5.2.2.2. | R |  | Dealt with in Annex J 7.1.8 |
| 6.4.2.1 (2) | UK | 6.4.2.1 (2) EDIT this clause to a principle. | EA |  |  |
| 6.4.2.2 (2) | FR | (2) A Here, ‘deformations’ means those that would be calculated using the behaviour curves of the connections. The beam-to-column connections classified as rigid according to the criteria of 6.9.6 shall be considered as meeting this requirement. The 5% requirement may concern the elastic critical value Vcr of the total vertical load applied to the structure (as far as the latter may be determined more easily than the ultimate resistance). It should be reminded that the value Vcr is calculated with the initial stiffness of the connections (see 5.2.2.1(7)). | R |  |  |
| 6.4.2.2 | D D | - Rigid connections. - A rigid connection shall be so designed that its deformation has no significant influence on the distribution of internal forces and moments in the structure, nor on its overall deformation. (2) The deformations of rigid connections should be such that they do not reduce the resistance of the structure by more than 5%. (3) A connection in a laterally supported frame or in a laterally unsupported frame which satisfies the condition specified in (4) may be considered to be rigid compared to the connected beam, if the initial rotational stiffness of its moment-rotation- characteristic lies above the solid line on the appropriate diagram in figure 6.4.1. (4) The line given in figure 6.4.1(a) for laterally unsupported frame may be used only for frames in which every storey satisfies: Kb __ 0,1 Kc in which Kb is the mean value of Ib/Lb for all beams at the top of that storey Kc is the mean value of Ic/Lb for all columns in that storey where Ib is the second moment of area of a beam Ic is the second moment of area of a column Lb is the span of a beam (centre-to-centre of columns) Lc is the storey height for a column - 6.4.2.2. can be left out. | A-M R R |  | Part of re-write Dealt within Annex J |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 6.4.2.2 (2) | UK | 6.4.2.2(2) REVIEW this clause as the overall resistance of the structure cannot be determined without knowledge of the moment/rotation characteristics of the rigid connections used in the structure. As there is always a chance that the fabricator will want to use connections with different characteristics there could be complicated contractual problems with this clause. This is not strictly an application rule as it gives different requirements to the principle. | R R |  |  |
| 6.4.2.3 | FR | A When the variable character of the actions may lead to sign inversions of a moment in connections which are heavily stressed in their non-linear range, the adaptability of the structure shall be checked until its ultimate limit state is reached, thus being an exception to clause 5.2.1.4(11). For want of a procedure, it shall be checked that when the semi-rigid connections are replaced with pinned- connections, the structure does not turn into a mechanism. | R |  | Negates purpose of rigid connections. |
| 6.4.2.3 | D | 6.4.2.3 Semi-rigid connections. (1) A connection which does not meet the criteria for a rigid connection of a nominally pinned connection given in 6.4.2.2(1) and 5.4.2.1(1) shall be classified as a semi-rigid connection. 6.4.3 Classification by strength 6.4.3.1 Nominally pinned connections |  |  |  |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 6.4.2.3 Cont’d | D CH | (1) A nominally pinned connection shall be capable of transmitting the calculated design forces without developing significant moments which might adversely affect members of the structure. (2) A connection may be classified as nominally pinned if its design moment resistance MRd, provided that it also has sufficient rotation capacity. - 6.4.2.3 can be left out. | A-M R |  | Part of re-write |
| 6.4.3.1(2) | UK | 6.4.3.1 (2) CLARIFY this clause BECAUSE it is not certain if the plastic hinge can form at the joint or if this is a requirement in a member which has a plastic hinge at some point. As it is in a pin joint it is assumed that the plastic hinges form in the members. If the structure is designed as a pinned connection type of structure then plastic hinge rotation will not be required. It is assumed that this clause intends that there should be sufficient rotation capacity in the joint for the plasticity in the beams at failure. This needs to be clearly stated. There appears to be a different meaning to the term plastic hinges in various countries, perhaps a full definition would help here. | R E,A |  |  |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 6.4.3.2 Cont’d | D | 6.4.3.2 Full Strength Connections (1) The design resistance of a full strength connection shall be not less than that of the member connected. - Where the rotation capacity of a full strength connection is limited, overstrength effects should be taken into account. If the design resistance of the connection is at least 1.2 times the design plastic resistance of the member, the rotation capacity of the connection need not be checked. 6.4.3.3 Partial strength connections. - The design resistance of a partial strength connection shall not be less than that necessary to transmit the calculated design forces and moments, but may be less than that of the member connected. - The rotation capacity of a partial strength connection which occurs at a plastic hinge location shall not be less than needed to enable all the necessary plastic hinges to develop under the design loads. | A-M |  | Part of re-write |
| 6.4.3.2 | D | - The principles for the determination of the connection properties given in 6.4.1 can be satisfied by following the detailed application rules given in Annex J. - The design of other types of connection not covered in Annex J should be based on similar application rules conforming to the principles given in section 6.4. - Alternative application rules can also be used provided that: - they accord with the same principles and - it can be demonstrated that they lead to at least the same safety level. | A-M |  | Part of re-write |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
|  |  | Figure 6.4.1 Recommended classification boundaries for rigid beam to column connections. | R |  | For plastic design criteria of nature of joint is strength. For Elastic design criteria of nature of joint is stiffness. In part 1.8 (c.f Annex J). Definititions of 1) Rigid 2) Semi-Rigid 3) Pinned Conceptual decision for 1) 2) or 3) This is a Semi-Rigid approach. |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 6.4.3.2 (1) | CH | 6.4.3.2 (1) can be left out. (2) should be transferred to 5.2.1.4 | R R |  |  |
|  | FR UK | - Full strength connections. The 1.2 factor may be justified on the basis of a probability calculation, which ensures that the plastic hinge does occur within the member. (2) A This factor shall be reduced to 1.0 in the case of full penetration butt connections. 6.4.3.2 (2) (3) EDIT These clauses are not applicable rules but additional requirements. REVIEW whether the factor 1,2 needs to be applied to the whole joint, or only to the non- ductile components such as bolts in tension and transverse welds. Also review whether the value 1,2 is sufficient to cover the overstrength (up to at least 1,5) possible in practice. | A R A |  | Comment only. |
| 6.4.3.3 (1) | FR | - Partial-strength connections. (1) C The concept of partial-strength connection allows the formation of plastic zones within the connection. During global analysis, when the design resistance of the connection is reached, its behaviour may then be considered as that of a plastic hinge. |  |  | Comment only |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 6.4.3.3 (1) | FR | (1) I Clause (1) must be invalidated and replace with The design resistance of a partial-strength connection is automatically less than that of the connected member. However, it shall not be less than the resistance which is necessary to transmit the design internal forces and moments. | E.A |  |  |
| 6.4.3.3 (2) | FIN | - Partial strength connections - The required rotation capacity should be defined if possible by simple way. | R |  | Impossible |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 6.5.1 | DENMARK | 6.5.1 EC3 is lacking rules for distances when edges and row of fasteners are neither in the direction of the force nor perpendicular to the force. For edge distances DK proposes to determine e1 and e2as the semi-axis in the ellipse with the plate edge as tangent and similarly for rows of fasteners p1 and p2 as the semi-axis in the ellipse with centre in the one hole and through the other hole, ref. the figure. | R |  |  |
| 6.5.1.1.(1) | UK | 6.5.1.1.(1) Edit this clause as the location of the bolts will not prevent corrosion, it can, with other suitable detailing, reduce the risk | E.A. |  |  |
| 6.5.1.1.(2) | D | (45) Add to clause (2) of 6.5.1.1. “… rivets and pins.” | E.A. |  |  |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 6.5.1.2 | FI | 6.5.1.2. Minimum end distance In the figure 11.2.6(case b dimension a) of prENV 1090-1 it is given that the permitted deviation of the position of the holes can be  = ± 5mm. Lets assume that we have the permitted deviation - 5mm. Lets assume, that the designer makes the following calculation: d = 12mm dO = 13mm e1 = 1,2 d = 1,2*13 = 15,60mm = e1/3dO = 15,6/(3*13) = 0,400 The bearing resistance is: Fb.Rd = 2,5*0,400*fu d t/m According to the prENV 1090-1 the following situation is allowed (taken into account the permitted deviation of -5mm) in the real structure: e1 = 15,60 - 5 = 10,60mm (-5 mm is allowed in the real structure)  = e1/3dO = 10,60/(3*13) = 0,272 The resistance in the real structure is: 100*(0,400 - 0,272)/0,400 = 32,0% lower than assumed by designer. This kind of minus tolerances have probably not been taken into account in the safety factors. I think this should be noted in EC2 and not to allow such minus tolerances for this kind of cases. | P |  | JBS to attempt to get 1090 altered. |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 6.5.1.2.(2) | FR CH UK | 6.5.1.2. Minimum end distance. (2)A In the case of preloaded high-strength bolts, the minimum end distance shall not be less than 1.5 dO. 6.5.1.2 (2) p 141 The bearing resistance can also be increased with a larger bolt diameter. New Proposal: “The bearing resistance can be increased for larger end distances see 6.5.5 and 6.5.6” 6.5.1.2. EDIT these clauses for consistency. | R A-M A |  |  |
| 6.5.1.3. | UK | 6.5.1.3 The first gives a minimum end distance (1.2dO) then states that to get the full bearing capacity it should be increased. The second gives a minimum edge distance (1.5dO) then states that this may be reduced providing that the bearing value is reduced. It would be clear if both clauses stated the minimum then pointed out that a higher value of bearing resistance could be obtained if a larger value of end or edge distance were used. The reverse approach would be equally acceptable. | A |  |  |
| 6.5.1.3 (2) | FR | 6.5.1.3. Minimum edge distance. (2)A In the case of preloaded high-strength bolts, the minimum edge distance shall not be less than 1.5dO. | R |  |  |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 6.5.1.4 6.5.1.5 | FR | 6.5.1.4. Maximum edge and edge distances. (1)+(2)C The stated specifications are shown on the following figures. By definition : t1  t2 and t = t2 If exposed to weather e1  40 mm + 4t or corrosion e2  40mm + 4t Otherwise: e1  12t or 150mm e2  12t ot 150mm (3)A The rule of an edge distance not exceeding 12t of 150mm, whichever is the larger, defined in (2) may not prevent local buckling. Since the connection at the row of fasteners is not continuous, the width-thickness ratio values of table 5.3.1. (sheet 3), which are specified for rolled sections according to the class of the plate, should be used, multiplied by a 0.8 reduction factor. 6.5.1.5 Minimum spacing (1) A In the case of preloaded high-strength bolts, the minimum value of p1 shall not be less than 3do. (2) In the case of preloaded high-strength bolts, the minimum value of p2 shall not be less than 3do. | R R R |  |  |

| # Clause No | ## Country | ### Remarks and comments |  |  |  | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6.5.1.8 | FR | 6.5.1.8. Slotted Holes C Summarised table for the positioning of holes for bolts and rivets. |  |  |  |  |  |  |
|  |  |  |  |  | Connection | E, A-M |  |  |
|  |  |  |  |  | Outer/Inner Plate |  |  |  |
|  |  | End Distance e1 |  |  | 1.2 do (1) 12t or 150mm (2 ) (max) |  |  |  |
|  |  |  |  |  |  |  |  |  |
|  |  | Edge Distance e2 |  |  | 1.5 do (3) 12t or 150mm (2) (max) |  |  |  |
|  |  |  |  |  |  |  |  |  |
|  |  | c/c spacing p1 | Outer row Compression member |  | 2.2 do (4) 14t or 200mm (6) (min) |  |  |  |
|  |  |  |  |  |  |  |  |  |
|  |  |  | Inner Row Compression member |  | 2.2 do (4) 14t or 200mm (6) (min) |  |  |  |
|  |  |  |  |  |  |  |  |  |
|  |  |  | Outer row Tension member |  | 2.2 do (4) 14t or 200mm (5) (min) |  |  |  |
|  |  |  |  |  |  |  |  |  |
|  |  |  | Inner row Tension member |  | 2.2 do (4) 28t or 400mm (5) (min) |  |  |  |
|  |  |  |  |  |  |  |  |  |
|  |  | c/c spacing p2 | Compression member |  | 3 do (7) 14t ot 200mm (6) (min) |  |  |  |
|  |  |  |  |  |  |  |  |  |
|  |  |  | Tension member |  | 3 do (7) |  |  |  |
|  |  | do = hole diameter t = thickness of the thinnest outer plate (1) This minimum end distance shall be increased if it is necessary to achieve adequate strength in relation to the bearing resistance, see 6.5.5.and6.5.6. 1.5 do for preloaded high-strength bolts. |  |  |  |  |  |  |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 6.5.1.8. (cont.) | FR | (2) The greater of the two values. If exposed to weather or corrosion : 40 mm + 4t (3) This distance may be reduced to 1.2do provided that the design bearing resistance is reduce accordingly, as stated in 6.5.5 or 6.5.6. 1.5do for preloaded high-strength bolts. (4) This distance shall be increased when it is necessary to achieve adequate strength compared with the bearing resistance, see 6.5.5.and6.5.6. 3do for preloaded high-strength bolts. (5) The smaller of the two values. This value may be multiplied by 1.5 if the members are not exposed to weather nor to corrosion. (6) The smaller of the two values. The centre-to-centre spacing of the fasteners shall not exceed the maximum value required to avoid local buckling between fasteners, either. (7) This c/c spacing may be reduced to 2.4do if the design bearing resistance is reduced accordingly, as stated in 6.5.5. or 6.5.6. 3do for preloaded high-strength bolts. In addition, in tension members, the c/c spacing p2 shall remain lower than the smaller of the two values 14t or 200mm. | E. A-M |  |  |
|  | UK | 6.5.1.8 EDIT this clause with a reference to clause 7.5.2 (9), which gives the limits for long and short slotted holes | R |  | Different issues. |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 6.5.2.1 | FR | 5.5.2.1 General (1) The definition of oversize holes is given in 7.5.2.6. The design method for compression members is stated in 5.4.4 |  |  | Comment only |
| 6.5.2.2.(1) | FR | 6.5.2.2. Design shear rupture resistance (1) C On figure 6.5.5, the relevant ‘block’ appears hatched and represents the part “torn off” during failure. Tensile failure occurs along the horizontal limit of the block, and shear plastic yield occurs along the left vertical limit of the block. |  |  | Comment only |
|  | UK | 6.5.2.2 PROVIDE additional rules for block tension and for the design of gusset plates etc. | A |  | In Annex J Validation Group. |
| 6.5.2.2 (2) (3) | CH | 6.5.2.2 (2) p145 Delete. Integrate formula (6.1) with the (3) following adaptions in figure 6.5.5 Veff,R3=[Anei,G.0.8.fu+Anei.Ify/3 ] l/m | P |  | Validation Group |
| 6.5.2.2 (1) (3) | FIN | 6.5.2.2 Design shear rupture resistance (1) The second sentence should reworded, because there are used words “tensile rupture” and the design formula (6.1) is basically based only for shear. (3) For the case “two rows of bolts” it should be k = 1,5 not 2,5? | P |  | Validation Group |
| 6.5.2.3 (2) | FR | 6.5.2.3 Angles connected by one leg (2) A Expression (6.4) is applicable to the case of 3 bolts or more. | E/A |  |  |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 6.5.2.3 (3) | NETH | 6.5.2.3. (3) Why is this clause needed? The buckling resistance had nothing to do with the design resistance of the cross section. | E/A |  |  |
| 6.5.2.3 | UK | 6.5.2.3 EDIT the heading to reflect the fact that members other than angles are included in (1). 6.5.2.3 DEVELOP this clause to include lug angles, angles connected back to back etc. More detail is required for channels and T’s. | E/A A |  |  |
| 6.5.2.3 (2) (3) | UK | 6.5.2.3 (2) & REVIEW these two clauses taking the following (3) into account: If clause (2) applies to both compression and tension members it should be noted that for compression members ‘d’ is to be taken as zero and Aoct as equal to the gross area. Clause (3) suggests that the formulae in sub clause (2) should use Aoct for compression members. If this is to there is inconsistency with 6.5.2.1(1), which states that fastener holes may be ignored in compression members. | R P |  | Over detailed Validation Group |

| # Clause No | ## Country | ### Remarks and comments |  |  |  |  |  |  | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Table 6.5.1 | D | (46) Table 6.5.1 should be redrafted |  |  |  |  |  |  | P P |  | Validation Group |
|  |  | Table 6.5.1 Reduction factors B2 and B3 |  |  |  |  |  |  |  |  |  |
|  |  | Pitch P1 |  |  |  0,25 do |  |  5,0 do |  |  |  |  |
|  |  | 2 bolts B2 |  |  | 0,4 |  | 0,5 |  |  |  |  |
|  |  | 3 bolts or more B3 |  |  | 0,5 |  | 0,7 |  |  |  |  |
|  |  | (47) In particular base connections the Hertz pressure should be checked. Therefore resistance values for the Hertz pressure should be given. A proposal is enclosed : |  |  |  |  |  |  |  |  |  |
|  |  |  |  | Material |  | fH,k in N/mm² |  |  |  |  | Rejected but consider for 6.5.13 (pinned connections) |
|  |  |  | 1 | S235 |  | 800 |  |  |  |  |  |
|  |  |  | 2 | S275 |  | 900 |  |  |  |  |  |
|  |  |  | 3 | S355 |  | 1000 |  |  |  |  |  |
|  |  | The design resistance for Hertz pressure should be calculated as follows: fH,Rd = fH,k Ymo |  |  |  |  |  |  |  |  |  |
| Figure 6.5.5 6.5.3 | CH CH | Figure 6.5.5 p146 Only 2 sketches are needed to explain formula (6.1). More sketches are only confusing. 6.5.3 p149 For what reason are categories defined? |  |  |  |  |  |  | E R |  | for clarity |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 6.5.3.1 | SW | 6.5.3.1 We miss one category of bolted connections, preloaded bolts subject to shear but not designed as slip resistant. This category has a very good resistance to fatigue if the load does not change direction. In this situation the fatigue resistance can safely be taken as the same as the fitted bolts. | A - M |  |  |
| 6.5.3.1 (2) | FIN UK | 6.5.3.1 Shear connections (2) Are 4.6 bolts also called “high strength bolts” as it is given? As “high strength bolts” only bolts with grade 8.8 or higher should be defined. 6.5.3.1 (2) EDIT the term “ordinary” and “high strength” bolts BECAUSE these terms can be confusing as both terms have different meanings in popular usage. It would be clearer simply to use the grade as a means of definition i.e. 4.6 to 10.9. | E, A - M E, A |  |  |
| 6.5.3.1 (4) | CH UK | 6.5.3.1 (4) p149 Why has the design bearing resistance to be verified for that type of connection? 6.5.3.1 (4) DELETE the reference to clause 6.5.5 BECAUSE in this case there is no need for a check on the bearing value, as the bolts will not go into bearing at ultimate load. | P P |  | Validation Group Validation Group |
| 6.5.3.2 | FR | 6.5.3 Categories of bolted connections 6.5.3.2 Tension connections (2) Category D with non-preloaded bolts corresponds to a behaviour concept, which is not covered in French standard NF P22-460. However the use of this category is justified if: |  |  |  |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
|  |  | (2) C - the connection is designed on the basis of an ultimate resistance analysis of the plastic type; - the behaviour of the connection beyond the serviceability limit state may be assessed with sufficient accuracy to allow its classification as ridged, semi-ridged, or possibly pinned (see Annex J). |  |  |  |
|  |  | (3) C Experience has clearly established that: a) preloaded bolts have but little influence on the connection stiffness beyond a certain dimension, b) preloaded bolts do not increase the ultimate resistance of the connection, c) the detailings which increase the fatigue strength are those which most reduce the prying forces and, consequently, the stress variations within the bolts. This observation is shown on the figures below: |  |  | Commentary No action |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 6.5.4 (1) | FR CH | 6.5.4 Distribution of forces between fasteners (1) This proportional distribution only relates, on fig. 6.5.7 (a), to the moment. The shear forces are evenly distributed between the fasteners. 6.5.4 (1) p151 Test have shown, that also shear deformations in bolts allow a plastic redistribution of forces. | P |  | Commentary no action Validation Group |
| 6.5.4 (2) | FR | (2) 1 This plastic distribution of forces in figures 6.5.7 (b), (c) and (d) may not be allowable in some situations. These figures are therefore invalidated. They may be replaces with the following plastic design method: A distribution of stresses is adopted, with stresses all equal to Fb,Rd, whose orientation varies progressively through the existence of a rotation centre O, of coordinate ro, as shown on the following figure. The internal forces and moments (MSd,/VSd, the solution of the system | P |  | Validation Group |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
|  |  | VM.Rd=roFb.Rd1 i ri VM.Rd(e+ro) = Fb.Rd1 i ri gives both ro and VM.Rd which is the design shear resistance in presence of moment MSd. It is then sufficient to check that: VSd VM.Rd |  |  |  |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 6.5.5 | UK | 6.5.5 EDIT the heading to “Design resistance of bolts in bearing type connections”. | A |  |  |
| 6.5.5 (4) | CH | 6.5.5 (4) p153 Can be simplified to: “If tp  0.5d, the punching shear resistance Bp.Rd has to be verified. In this form you realise directly, that in 99% of practical cases no check for punching shear has to be made. | A - M |  |  |
| 6.5.5 (2) | FIN | 6.5.5 Design resistance of bolts (2) Can the bearing resistance for individual bolts be added together or not? Some clarification is needed in the text. See the figure and example below: |  |  |  |
| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
|  |  | For the holes 2 we get: a = eI/3dO = 1,2dO/3dO = 1,2/3 = 0,4 For the holes 1 we get: a = P1/3dO-0.25 = 3dO/3dO - 0,25 = 1 - 0,25 = 0,75 Is the total bearing resistance: (resistance is based in direct summarising). Fb.Rd = ( a) (2,5 fu d t/YMb) = (2*0,4 + 2*0,75) * (2,5 fu d t/Ymb) (Method 1) or (Resistance is based on smallest of the individual resistance’s) Fb.Rd = ( a) (2,5 fu d t/YMb) = (2*0,4 + 2*0,40) * (2,5 fu d t/Ymb) (Method 2) If the method 1 is the right one then the deformation in the holes 2 can be quite high also at serviceability limit state if all loads are permanent load. | P |  | Validation Group |
| 6.5.5 (3) | UK | 6.5.5 (3) INSERT a reference to 6.5.9, which is required for forces due to prying action. | A |  |  |
| 6.5.5 (5) | FR | 6.5.5 Design resistance of bolts (5) C More precisely, the four following requirements shall be met: |  |  |  |
| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
|  |  | Ft.Sd  1 , Ft.Sd + Fv.Sd  1 Ft.Rd 1,4 Ft.Rd Fv.Rd #### Ft.Sd  1 , Fv.Sd  1 Bp.Rd Fd.Rd |  |  | Comment only - no action |
|  | CH | 6.5.5 (5) p153 A bolt plastified by a tension force can still take a shear force of Fv,sd = 0.286 FvRd What is the technical background. A more logical proposal would be: 2 2 Fv.Sd + Ft.Sd  1 Fv.Rd Ft.rd | P |  | Validation Group |
| Table 6.5.3 | Austria Denmark Ireland | Tab 6.5.3 In the first row of table 6.5.3 (Design resistance for bolts - Shear resistance per shear plane) should As be replaced by A (twice) and A be replaced by As (once). Table 6.5.3 Strength grade 6.8 shall be added in the same category as 4.8, 5.8 and 10.9. Table 6.5.3 Design resistance for bolts The expression for bearing resistance of bolts gives exceptionally high values, making it almost impossible to design a cleated end connection (such as any of those shown in Figure 6.5.5) using plastic analysis, because the shear value of the bolts will invariably be less than the bearing value unless the web of the beam is exceptionally thin. | R A |  |  |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
|  |  | The very high value for bearing, no doubt derived from tests, may depend on the clamping action of the tightened bolt giving rise to containment of the plasticity of the parts joined when these are in close contact. If this is the case, it should not be relied upon, since in ENV1090.1, the new code for the fabrication and erection of structural steelwork developed by CEN/TC135, close contact between connected parts is not required, and a gap of not more than 2mm is permissible. A gap between the connected parts would eliminate any contribution to the bearing strength by containment. The expression for bearing strength of bolts should be reviewed to ensure that the tolerances allowed in the new fabrication code are taken into account | P |  | Validation Group |
|  | CH | Table 6.5.3 P154 Editorial error. Change As and A in the formulas. Add formula 6.5.5 (5) to this table. | R A |  |  |
|  | UK | MODIFY table 6.5.3 as follows - add grade 6.8 after 5.8 - replace the use of  by a list of table of the various criteria affecting bearing resistance, with a separate formula for each. | A |  |  |
| 6.5.5 (8) | France | (8) A Without a conclusive experimental justification, the first condition shall also apply to grade 8.8 bolts. | R |  |  |
| 6.5.5 (9) | CH | 6.5.5 (9) p155 This restriction is to strong for normal edge distances, measured in the direction of load transfer. A reduction of the bearing resistance due to e2 and/or p2 is only rectified for long end distances e and/or long spacings p. | P |  | Validation Group |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 6.5.5 (10) | UK | 6.5.5 CLARIFY the text in this clause by introducing formulae, which could be included in Table 6.3. | A/P |  | Validation Group |
| 6.5.5 (11) | Finland UK | (11) We propose to delete table 6.5.4 with associated text. There is not need to give in EN standard alternative conservative values. The basic design rules in table 6.5.3 are simple enough to use for everyone. 6.5.5 REVIEW the bearing stresses BECAUSE the resistance of bolts using the Eurocode rules will lead to potential problems where joint movement is critical, it is suggested that in the final EN the values are reduced. Where movement in a joint is not critical then higher stresses may be permitted. The UK can supply values which could be adopted as they are based on a joint movement small enough not to change design assumptions. | A A |  |  |
| Table 6.5.4 | CH | Table 6.5.4 p 155 Can be left out. Either you calculate the bearing resistance due to the appropriate formula or you take the value direct from a more detailed design aid table. | A |  |  |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 6.5.6 | Sweden | 6.5.6 There is no need for new steel structures, so please delete. 6.5.6 p156 Leave out. If necessary the designer will use literature or an old design code. 6.5.6 REVIEW the use of rivets which have been included in the ENV are they needed in the final EN version of the Eurocode? | R R R |  |  |
| 6.5.6(1) | France | (1)C The design resistance values in this clause relate to rivets in conformity with Reference Standard 5 of Annex BB. |  |  | Comment only – no action |
| 6.5.7 | UK | 6.5.7 PROVIDE requirements for the punching resistance of countersunk bolts and rivets in this section, to match those for countersunk bolts in tension, see 6.5.5.(4). REVIEW the need to apply the 0.7 factor to a countersunk bolt. It is believed that it is relevant only to rivets. | R/P A/P |  | Validation Group “ |
| 6.5.7.(3) | UK | 6.5.7 (3) REVIEW the need to deduct half the thickness. If the rule is valid at all, it is presumably valid only for certain bearing criteria. | P |  | “ |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 6.5.8 | UK | 6.5.8 PROVIDE a statement that the bolts will need to be checked for shear. BECAUSE category B bolts will, in these circumstances, be acting as bolts in clearance holes once slip has taken place between serviceability and ultimate loads. | R |  |  |
| 6.5.8.1 (1) (2) | FIN | 6.5.8.1 Preloading? Slip Resistance (1) Is the definition of “high strength bolts” self-evident. Compare also clause 6.5.3 (2) (2) Are the ks -values intended to be used unindependent of the direction of the applied load? | E E |  |  |
| 6.5.8.1 (3) | FR UK | 6.5.8 High-strength bolts in slip-resistant connections 6.5.8.1 Slip resistance (3) I The values of ms to use are as follows: ms ult = 1.10 and ms = 1.20 6.5.8.1 (3) EDIT to recognise that EC3 specifies 3 levels of loads for serviceability limit states REVIEW the recommended muer values and MODIFY in line with NADs. | E |  | Comment only - no action |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 6.5.8.1 (4) | FR | (4) I In these particular cases of connections, the following value shall be used. ms ult = 1.25 |  |  | Comment only – no action |
|  | CH | 6.5.8.1 (4) p 158 With an appropriate formulation the definition “Category C” is not necessary. |  |  |  |
| 6.5.8.2 (2) | UK | 6.5.8.2 (2) PROVIDE guidance on the design preloading force to be used, which the engineer can use in his design. These should be based on the type of bolt and fittings. | R |  | Preload given |
| 6.5.8.3 | CH | 6.5.8.3 p 159 Make reference to ENV 1090, Annex A. | E |  |  |
| 6.5.8.3 (1) (2) | CH CH | 6.5.8.3 (1) p 159 Could be eventually simplified with a table. (3) | E |  |  |
| 6.5.8.4 (1) | FR CH | - Combined tension and shear. (1) C When tension and shear are combined, the preloading force Fp is not reduced by the whole tensile force Ft applied externally. Among others, the stiffness ratio between the tensile bolt and the compression plates (of about 1 to 4) results in a contact force remaining between the plates, at least equal to: Fc=Fp – 0.8 Ft When the force Ft is applied, in the usual conditions Delete the reference to Category B and C. | R |  | Comment only – no action |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 6.5.8.4 (1) Cont’d | UK | 6.5.8.4 (1) REVIEW the validity of the 0,8 factor. It is based on an assumed cylinder in compression with a fixed area, whereas finite element studies indicate a “barrel of compression such that the factor should be a function of the thickness, and possibly of the bolt grade, steel grade and number of plies. Old British studies found that the value can be as high as 0,95 in practice and concluded that 1,0 should be used for design, which is also American practice. | P |  | Validation Group |
| 6.5.8.4 (2) | UK | 6.5.8.4 (2) REVIEW this clause BECAUSE the contact area has been shown to be an annular zone around the bolt hole. Evidence is required to show that the lower contact pressures over a distributed area will be as effective as very high stresses in local areas. It should also be demonstrated there will be no loss of effectiveness due to corrosion or distortion of the plies. | P |  | Validation Group |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 6.5.9 (2) | FR | 6.5.9 Prying forces (2) C Prying forces depend on the relative stiffnesses between bolts and T-parts only when the connection behaves in the elastic range. Standard NF P 22-460 and DTU P22-701 (CM66) - article 4.03 - are rather intended to limit the deformations of the connection and, consequently, to keep these prying forces within negligible values. |  |  | Comment only – no action |
| 6.5.9 (3) | FR | (3) C The prying forces integrated in the design model of Annex J are considered within a concept of ultimate limit resistance of the connection, therefore different from the concept of the comment to clause (2). The external force FtRd per bolt is then inferred from the analysis of the various plastic mechanisms which may occur in the connection. |  |  | Comment only – no action |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 6.5.10 (1) | FR UK | 6.5.10 Long joints (1) C It should be noted that the reduction of the resistance due to the length of the connection does not apply in the case of bearing resistances Fb.Rd < Fv.Rd, nor in the case of slip- resistant connections. 6.5.10 (1) EDIT the cross reference to apply to slip resistant connections and countersunk bolts. In fact it does apply to countersunk bolts and category B slip resistant connections at the ULS. | E |  | Comment only – no action |
| TABLE 6.5.6 | UK | Table 6.5.6 EDIT this as a figure and not a table. | A |  |  |
| 6.5.11 | CH | 6.5.11 p163 That kind of joint should be generally avoided. If nevertheless such joints are used, reference to the effect of (2) will satisfy. | A |  |  |
| 6.5.12 | DENMARK | 6.5.12 The rule in (1) is liberal and may lead to absurdities DK propose to re-examine the rule. | P |  | Validation Group |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| FIG 6.5.12 | UK | Figure 6.5.12 MODIFY as this would be clearer if it used variations on t (i.e ta, tb, etc) rather than a, b and c, for the thickness of, and gaps between, the plates. Note a and c are used in the previous figure for other dimensions. Figure 6.5.12 MODIFY the lower diagram which is, presumably the stress distribution on the various plies in the pin joint. This should be stated. | E E |  |  |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 6.5.13 | DENMARK | 6.5.13 The rules in EC3 seem very conservative. For bending a factor 0.8 is introduced and the high partial safety factor Mp is used for the yield strength. DK propose the rules to be re-examined and that the rules are only used if rotation is required under full loading. Add after 6.5.13.1 (1): (P) The requirements in the following should be met if the function of the connection demands that it is to rotate freely in the ultimate limit state, i.e. when subjected to the design force Nsd. (A) If the free rotation is relevant only for small actions the connection may be taken as a bolted connection with one bolt. | E |  | Validation Group |
| 6.5.13 | UK | 6.5.13 CLARIFY which of the three possible sets of criteria for pins the rules given are intended to address. In some structural details it is necessary for the connected members to rotate slightly on the pin, whereas in others it is simply a peg. Also in some structures the intention is to be able to remove and replace the pin during demounting and reassembly, whereas in others it is in place “permanently”. | P |  | Validation Group |
| 6.5.13.2 (1) | FR | 6.5.1.3.2 Pin holes and pin Plates (1) A This clause must be considered as an Application Rule and not as a Principle. | E |  |  |
| 6.5.13.2 (2) | UK | 6.5.13.2 (2) EDIT the reference should be to 6.5.5 | R |  |  |
| 6.5.13.2 (3) | CH | 6.5.13.2 (3) p 164 Not very clear. A sketch would help. | A-M |  |  |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 6.5.13.3 (1) | FR | 6.5.13.3 Design of pins (1) A This clause must be considered as an Application Rule and not as a Principle. | E |  |  |
| 6.5.13.3 (2) | UK | 6.5.13.3 (2) DEVELOP this clause to cover the following: No mention has been made about the effects of phosphor bronze or similar inserts and their effect on the bearing strength of the joint. This should be covered, even if it is by means of a reference to the bridge part, when published. | A-M |  |  |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 7.1.1 (3) |  | 7 Fabrication and erection 7.1 General 7.1.1 Scope (3) 1 This clause is not applicable in this paragraph. It must be transferred, substantially, into 7.2. | E |  | # CONSIDER ALL THIS WHEN RE-DRAFTING |
| 7.1.2 | FR | 7.1.2 Requirements 1 All the contents of this paragraph must be conveyed into 7.2 which is the right place. | E |  |  |
| 7.2 (1) | FR | 7.2 Project Specification I Clauses of paragraph 7.2 contain some relational aspects. We propose the following clauses: (1) The Project Specification shall include the minimum requirements stated in paragraphs 7.3 to 7.7. (2) The requirements of the Project Specification shall not be below the minimum requirements of this section. (3) The minimum Project requirements shall be specified in terms of the Reference Standards stated in Annex B. (4) The specific requirements for special structures shall be included in the Project Specification. | E |  |  |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 7.2 (1) Cont’d | FR | 7.2 Project specification Cont’d… (5) As much as possible, the special requirements of the Project Specification shall be stated in accordance with the Reference Standards. | E |  |  |
|  |  | 7.3 Fabrication restrictions I We propose to replace the paragraph 7.3 with: (1) The use of hardened material shall be avoided or forbidden in some cases, and suitable provisions shall be made. This hardening may be due to strain or quenching. As concerns the limitations of sue, refer to: - Reference Standard 6, as a general rule. - Section 9, when fatigue is a limit state to be considered. - the restrictions that shall be defined in the Project Specification, in special cases. | E |  |  |
| 7.4 (4) | UK | 7.4 (4) EDIT to refer to the requirements of ENV 1090. | A |  |  |
| 7.5.1 | ITALY | 7.5.1 Holes Add the following provision to paragraph (19) of 7.5.1 of EC3: The use of a flame in processing holes is always excluded. | A/E |  |  |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 7.5.1 (2) | UK | 7.5.1 (2) EDIT to refer to ENV 1090 for punching. | A |  |  |
| 7.5.1 (3) (4) | FRANCE | 7.5.1 Holes I Clauses (3) and (4) are to be deleted in the expectation of the specific European Standards. | R |  |  |
| 7.5.2 | DENMARK | 7.5.2 Clearance for fitted bolts should be specified. | A |  |  |
| 7.5.2 (4) | FR | 7.5.2 Clearances in holes for fasteners. (4) I Clause (4) must be replaced with: The clearances for fitted bolts shall in no case exceed 0.3mm. | A-M |  | See ENV 1090 – 5 |
| 7.5.2 (8) | FR CH | (8) C To make erection easier and allow the alignment of the structure, taking into account imperfections and cumulative tolerances, the holes in the base plates may be oversized to a considerably greater diameter than that of the bolts. 7.5.2 (8) p 202 Make reference to 7.7.5 (3). | E |  | Comment only – no action |
| 7.5.2 (9) (10) | FINLAND | 7.5.2 Clearance in holes for fasteners (9) and (10) The presentation of sizes could be more clear like the presentation in prEN 1090-1. A clear figure could be added. | E |  |  |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 7.5.2 (12) | FR | (12) C Slotted holes consist of two semi-circles with a same diameter, joined together by two parallel faces with a spacing equal to the diameter value (see 7.5.1(5) for clotted hole forming). The centre-to-centre distance between semi-circles shall be adjusted according to the required displacement amplitude. In addition, the tightening of bolts shall be moderate in order to allow the required operation. This implies a nut-stopping device. |  |  | Comment only – no action |
| 7.5.3 (3) (4) | UK | 7.5.3 (3) & (4) EDIT in line with the agreed rules for ENV 1090-1 | A-M |  | Make reference only. |
| 7.5.5 | UK | 7.5.5 EDIT to ensure that washers are provided where a protection system has been applied to prevent damage to the system. | R |  | (EN1090) |
| 7.5.6 (3) | FR | 7.5.6 Tightening of bolts. (3) C The relevant standards of Reference Standard 8 are standards NF P 22-464, NF P 22-464, NF P 22-466, NF P 22-468 and P 22-469. |  |  | Comment only – no action |
| 7.5.8 (1) | FINLAND | 7.5.8 Fit of contact surfaces (1) It is really true that also in categories B, C and also E the gap of 1mm can be allowed? It should be given if this gap is measured before or after tightening of bolts. On the other hand 2mm gap can be dangerous in outdoor conditions if moisture is present and crevice corrosion can occur. | R |  | Corrosion not the issue. |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 7.6 (1) | UK | 7.6 (1) EDIT to refer to ENV 1090. | A/E |  |  |
| 7.7.3 | UK | 7.7.3 EDIT in line with ENV 1090. Tolerances should only be changed for special structures or when there is a particularly good reason, i.e. fixing special cladding. | A/E |  |  |
| 7.7.3 (3) | CH | 7.7.3 (3) p 207 not consistent with ENV 1090-1 11.4.1. | A/E |  |  |
| 7.7.4 (1) | FR | 7.7.4 Fabrication tolerances. (1) A Until the publication of the European pre-standard about the construction of steel structures falling within the competence of the Technical Committee (CEN TC/135), the Project Specification shall provide all the needed requirements, in conformity with the design rules, and, as far as possible, drawn from the latest version of the draft of this pre- standard. | A |  |  |
| 7.8 | UK | 7.8 EDIT to cover the change to ENV 1090. | A |  | Comment |
|  | FR | 7.8 Inspection and testing C Among the standards stated here, standard NF P 22-473, NF P 22-464, NF P 22-466, NF P 22-468 and P 22-469 shall be referred to as concerns ‘Inspection and Testing’ aspects. |  |  | Comment only – no action |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 8.1.(2) | FRA | 8 Design assisted by testing 8.1 Basis (2)C It is always advisable to use a theoretical behaviour model. However, for some particular productions, an experimental determination of the resistance may be used without resorting to a theoretical model as stated above. The procedures described in Annex Y should then be referred to, for the test planning and procedures, as well as for the test evaluation. |  |  | Comment only – no action |
| (3) | FRA | (3)C It is therefore the responsibility of the person in charge of the tests to list all the factors which are likely to affect the behaviour of the analysed product or system, including those which are contractually allowed for in the calculation models. |  |  | Comment only – no action |
|  | UK | 8.1 (3) Because experimental work is undertaken it will often be found that the rules given in a design code are conservative, simply because they have to cover all eventualities. If specific areas are addressed in tests then there will be a saving, which must be allowed, if there is to be any benefit from testing. EDIT the restriction on bypassing calculations to cover: 1) factors of safety should be not less than those required from Chapter 2. 2) the resistance of the structure should be determined from the rules given in Annexes Y or Z, for the interpretation of test results, or some other equally reliable source. 3) the strength of the relevant components in the final structure shall not be extrapolated beyond the range of tests. | A/E |  |  |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| 8.2(5)(e) | FRA | 8.2 Planning of tests (5)(e)C ‘Loading path’ means the evolution of the loading in time and space (in time, e.g. step-loading, in space, e.g. application of moving loads). |  |  | Comment only – no action |
| 8.4.(1) | FRA | 8.4 Test evaluation (1)C ‘Data’ means the random variables used in the formulation of Annex Z (basic variable and model correction variables). |  |  | Comment only – no action |
| 8.5.(1) | FRA | 8.5 Documentation (1)A The documentation may more particularly include comments on all the incidents which occurred during the tests. It may also possibly include an interpretation of the results. | R |  |  |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| Annex Y | UK | #### Annex Y General TRANSFER into the revised Chapter 8. Items not covered in Eurocode 3 1-1 required by designers. Portal Frames No rules for the design of portal frames have been included. Some mention has already been made of this point. The following items require attention: 1) Stability of frames with sloping members 2) Snap through stability of rafters 3) Stability of members with tapered cross sections 4) Stability of members in bending, restrained on the tension flange 5) Design of connections between haunched beams and columns Members restrained on the tension flange No rules have been provided for the design of members in bending with or without axial load with restraint on the tension flange. Detailed rules have been prepared in the UK in our own national codes covering these points, in addition rules have also been prepared using the latest research, which will be sent to the Project Team to help with the development. | A |  |  |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
|  |  | Disproportionate collapse There are no provisions for dealing with disproportionate collapse of structures, some further guidance is required, possibly by requiring tying forces to be provided. This question is raised in a number of places within the Eurocode, especially in the clauses dealing with fatigue and brittle fracture. | A |  |  |
| Y.1 (1) (a) (2) (ii) (2)(iv) | France France France | Y.1 General (1)(a) Test (iii) may also be used (2)(ii) C The required ultimate load is the test load defined in paragraph Y.4.2 (7). This test load varies according to the design load at the ultimate limit state FSd.ult. (2)(iv) C Tests to failure may also be used to establish calculation models or strength formulae. This case is dealt with in paragraph Y.4.5. |  |  | Comment only – no action |
| Y.2.(4) | France | Y.2 Test Conditions (4) The accuracy of the measurements shall correspond with that required for correct test evaluation. |  |  | Comment only – no action |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| Y.3 (2) (3) (7) | France France France | Y.3 General test procedures (2) 1 Clause (2) is invalidated and replace with: Prior to any test, preliminary loading, not exceeding 30% of the characteristic values of the relevant loads, may by applied and then removed in order to bed down the test specimen onto the test rig. (3) C ‘Loading phase’ means any period during which the behaviour of the test specimen remains the same. In order to allow this comparison, all geometrical dimensions of the test shall also be measured. | R A |  | Comment only – no action |
| Y.4.1 (1) | Finland | Y.4.1 Acceptance test (1) We propose the following addition: In addition to the acceptance test it shall be verified for example by calculation that the safety level given in the Eurocode 3 is achieved. The reason for this addition are: - the design of structures can not be based only on acceptance test using the given safety factors. - somebody can imagine that the given safety factors are enough for design of the structure | A-M |  |  |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| Y.4.1 (3) (4) (a) | France France | Y.4.1 Acceptance test (3) C The values specified in the combination defining the test load are representative values. The authority in charge may specify different load levels to be applied. Should the case arise, several test loads, relating to various variable load combinations, may be defined. (3) I Clause (3) is invalidated and replaced with: The test load for an acceptance test shall be: - 1.0 x (actual self-weight of the tested structure or element) - 1.0 x (remainder of the loads), and - 1.0 x (variable loads) (4) (a) A The global behaviour shall be elastic up to the test loading. This behaviour is linear as a general rule, but not always so: | R R |  | Comment only – no action No Safety Margin |
| Y.4.1 (4) (b) | France | (4) (b) 1 Clause (4)(b) is invalidated and replaced with: On removal of the test load, the residual displacement shall not exceed 10% of the maximum value recorded during the test. | R |  | Too Severe |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| (5) | France | (5)1 Clause (5) is invalid and replaced with: If the conditions given in (4) are not satisfied, the loading may be applied a second time. The test specimen shall demonstrate elastic behaviour under this second application of the test loading, and the new residential displacement shall not exceed 5% of the maximum value recorded during this second test. | R |  |  |
| Y.4.2(1) (3) (4) (7) | France France France France | Y.4.2 Strength test, (1) C In the strength test a calculation model that allows a first evaluation of the design strength Rd is assumed available. The expression of Rd as a function of the geometric dimensions and of the mechanical parameters then allows the correction carried out in formula (Y.1). (3) C The strength test may be designed in such a way that it includes the acceptance test. (4) C Referring to the design load concept means that a specific use of the structure, or of the structure component, is referred to. (7) C Since the correction factor R(Gm, fvmes) uses the expression o R(Gn, fyn) of R as a function of G and fy, it is not necessary to use the average value fym assessed in Y.4.2 (6). Clause (7) assumes that the test specimen consists of components or parts with the same nominal yield strength. When the calculation model refers to several different nominal yield strengths, R(Gn, fyn) becomes (R(Gn, {fyni}). |  |  | Comment only – no action |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
|  |  | That will be, for instance, the case for the design crushing resistance of the web of an I, H or U hybrid section (see formula (5.72) of section 5, which explicitly includes the yield strengths fyt and fyw of the flange and of the web). (7) 1 Formula (Y.1) is invalidated and replaced with: Ftest.s = YMi FSd.ult R(Gm, fymes) i = 0,1,2 (Y.1) R(Gn, fyn) where : FSd.ult is the design load for the ultimate limit state, YMi is the partial safety factor relevant to the analysed limit state (YMO, YMI or YM2), Gn, fyn are the nominal values of the geometric dimensions and of the yield strength, Gm,fymes are the measured values of the geometric dimensions and of the yield strength of the various elements or parts of the test specimen. | P |  | Validation Group |
| Y.4.2 (9) | France | (9) C The test specimen, once submitted to the strength test, is unsuitable for use. If the residual displacement, on removal of the test load, exceeds the 80% threshold previously specified, the failure of the test specimen is then very nearly reached (see Y.4.3). |  |  | Comment only – no action |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| Y.4.3 (1) (7) | France France | Y.4.3 Test to failure (1) C As in the strength test, the general case is assumed to be the case where a calculation model is available. Nevertheless, the test to failure may be carried out without such a model. In this case, clause (11) of the invalidation of paragraph Y.4.3 shall be referred to. (7) C Reaching a previously defined limit deformation may be used for the conventional determination of the ultimate strength. 1 Clause (10) to (14) are invalidated and replaced with clauses (10) and (11) hereafter: (10) When the deviation from the mean does not exceed 10%, the design resistance shall be determined from clause (11) hereafter. (11) The design resistance FRd shall be determined from the behaviour of the test specimen during the test. Once the type of behaviour curve linking a force with a characteristic displacement of the test specification has been selected, the behaviour curve achieved shall be related to one of the four (case of members) or three (case of connections) shapes of previously defined experimental behaviour curves. Each of these shapes (numbered 1 to 4 on figures 1 and 2 hereafter) refers to an appropriate design resistance assessment formula. - In the case of members (fig, 1), the evolution from shape 1 towards shape 4 is from ductile-type failures to brittle type failures. | P |  | Comment only – no action Validation Group |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
|  |  | - In the case of connections (fig. 2), the evolution from shape 1 towards shape 3 is from elements with a high rotation capacity to elements with a low rotation capacity. ##### Design resistance assessment formulae Shape 1 Frd = 0,9 F test.R.min R(Gn, fyn) /YMi i = 0,1,2 (Y.2) R(Gm, fymes) Shape 2 Frd = 0,75 F test.R.min R(Gn, fyn) /YMi i = 1,2 (Y.3) R(Gm, fymes) Shape 3 & 4 Frd = 0,6 F test.R.min R(Gn, fyn) /YMi i = 1,2 (Y.4) R(Gm, fymes) In formulae (Y.2) to (Y.4) Ftest.R.min is the lowest test result YMi is the partial safety factor relevant to the analysed limit state (YMO, YMI or YM2) Gn, Fyn are the nominal values of the geometric dimensions and of the yield strength. Gm, fymes are the measured values of the geometric dimensions and of the yield strength of the various elements or parts of the test specimen.. |  |  |  |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
|  | FRA | ###### Case of members Figure 1 Typical behaviour curves for the design strength assessment in the cast of test to failure : case of members. Cast of connections Figure 2 Behaviour curves and u/el ratios for the design strength assessment in the cast of test to failure : case of connections. | P |  | Validation Group |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| Y4.3(7) cont. |  | Factors 0.9, 0.75 and 0.6 of formulae (Y.2),(Y.3) and (Y.4) have been established by taking various considerations into account. In some cases, they are meant to differentiate reliability : a higher safety level is assigned to limit states corresponding to brittle failure. In the case of several nominal yield strength, the comments to paragraph Y.4.2(7) shall be referred to as concerns the strength test. The test to failure may be used even if a theoretical model is not available. In this case, the correcting factor for formulae (Y.2) to (Y.4) shall be fyn/fym where fyn if the nominal value of the yield strength and fym is the average value of the yield strength such as defined in paragraph Y.4.2(6). In the case where the nominal yield strength is not single, the ratio fymi/ fyni shall be calculated for each nominal yield point fyni and the highest ratio shall be retained for the application of formulae (Y.2) to (Y.4). In this case, fymi is the average value of the yield strength of the elements or parts of the test specimen with a nominal yield strength fyni. |  |  |  |
| Y.4.5(1) | FRA | # Y.4.5 Testing to determine strength functions and model factors (1)C This is, for instance, the case of multiplicative strength formulae such as: R = bX11 X2 ….. Xp  2 p whose factors 1, …. p are assessed by multiple regression from test results. In this method, X1, X2 …. Xp are generally dimension less variables : the values found out for factors i are valid only within the scope of the variation ranges of variables Xi. |  |  | Comment only – no action |

| # Clause No | ## Country | ### Remarks and comments | Classif. |  | ### Proposed Action/Comment |
| --- | --- | --- | --- | --- | --- |
| Y.4.6(1) | FRA | # Y.4.6 Other test procedures (1)C Some test procedures are defined in other types of standards, particularly in test standards. |  |  | Comment only – no action |