- Laps, lapping length

- The transmission of the forces from one bar to the next must be assured.

- Possibilities:

- lapping of bars

- welding

- mechanical devices

- Lap length and anchor length are calculated from the design value of the ultimate bond stress, fbd, for ribbed bars may be taken as:

- fbd = 2,25 η1 η2 fctd

where:

fctd  is the design value of concrete tensile strength.  Due to the increasing brittleness of higher strength concrete, fctk,0,05 should be limited here to the value for C60/75, unless it can be verified that the average bond strength increases above this limit

η1   is a coefficient related to the quality of the bond condition and the position of the bar during concreting:

η1 = 1,0 when ‘good’ conditions are obtained and

η1 = 0,7 for all other cases and for bars in structural elements built with slip-forms, unless it can be shown that ‘good’ bond conditions exist

2    is related to the bar diameter:

2 = 1,0 for ø   32 mm

2 = (132 - ø)/100 for ø  > 32 mm

Lap length

Lap length depends on the shape of the bar, cover and spacing between bars, on presence of transverse reinforcement and transverse pressure forces. These effect could be implemented by factors α1 , α2 , α3, α4 , α5, α6 given in a code.

The design lap length is:

l0 = α1 α2 α3 α5 α6 lb,rqd   l0,min

where:

lb,rqd   is the basic required anchorage length calculated from

lb,rqd = (ø/ 4) (sd / fbd)

Where sd is the design stress of the bar at the position from where the anchorage is measured from.

l0,min > max{0,3 α6 lb,rqd; 15 ø; 200 mm}

Table - coefficients α1, α2, α3, α4 and α5

| Influencing factor | Type of anchorage | Reinforcement bar |  |
| --- | --- | --- | --- |
|  |  | In tension | In compression |
| Shape of bars | Straight | α1 = 1,0 | α1 = 1,0 |
|  | Other than straight (see Figure 8.1 (b), (c) and (d) | α1 = 0,7 if cd >3 otherwise α1 = 1,0 (see Figure 1for values of cd) | α1 = 1,0 |
| Concrete cover | Straight | α2 = 1 – 0,15 (cd –)/  0,7  1,0 | α2 = 1,0 |
|  | Other than straight (see Figure 8.1 (b), (c) and (d)) | α2 = 1 – 0,15 (cd – 3)/  0,7  1,0 (see figure 1 for values of cd) | α2 = 1,0 |
| Confinement by transverse reinforcement not welded to main reinforcement | All types | α3 = 1 – Kλ  0,7  1,0 | α3 = 1,0 |
| Confinement by welded transverse reinforcement* | All types, position and size as specified in Figure 8.1 (e) | α4 = 0,7 | α4 = 0,7 |
| Confinement by transverse pressure | All types | α5 = 1 – 0,04p  0,7  1,0 | - |
| where: λ = (Ast - Ast,min)/ As Ast cross-sectional area of the transverse reinforcement along the design anchorage length lbd Ast,min cross-sectional area of the minimum transverse reinforcement = 0,25 As for beams and 0 for slabs As area of a single anchored bar with maximum bar diameter K values shown in figure p transverse pressure [MPa] at ultimate limit state along lbd |  |  |  |
| For direct supports lbd may be taken less than lb,min provided that there is at least one transverse wire welded within the support. This should be at least 15 mm from the face of the support. |  |  |  |

Table: Values of the coefficient α6

| Percentage of lapped bars relative to the total cross-section area | < 25% | 33% | 50% | >50% |
| --- | --- | --- | --- | --- |
| α6 | 1 | 1,15 | 1,4 | 1,5 |
| Note: Intermediate values may be determined by interpolation. |  |  |  |  |

Figure 1: Values of cd  for beams and slabs

a) Straight bars	          b) Bent or hooked bars	       c) Looped bars

cd = min (a/2, c1, c)            cd = min (a/2, c1)                        cd = c

- Figure 2: Values of K  for beams and slabs

K = 0,1	           K = 0,05		       K = 0

Figure 8.4:

Laps for welded mesh fabrics made of ribbed wires

Laps of the main reinforcement

Laps may be made either by intermeshing or by layering of the fabrics.

Figure 3: Lapping of welded fabric

fig.: intermeshed fabric (longitudinal section)

fig.: layered fabric (longitudinal section)

For layered fabric, the laps of the main reinforcement should generally be situated in zones where the calculated stress in the reinforcement at ultimate limit state is not more than 80% of the design strength. (Avoid lapping in areas with high moments (forces).)

Laps of secondary or distribution reinforcement

All secondary reinforcement may be lapped at the same location.

The minimum values of the lap length l0 are given in a table bellow; the lap length of two secondary bars should cover two main bars.

- Table: Required lap lengths for secondary wires of fabrics

| Diameter of secondary wires (mm) | Lap lengths |
| --- | --- |
| ø  6 |  150 mm; at least 1 wire pitch within the lap length |
| 6 < ø  8,5 |  250 mm; at least 2 wire pitches |
| 8,5 < ø  12 |  350 mm; at least 2 wire pitches |