| Characteristic | POROTHERM 30 Profi Dryfix |
| --- | --- |
| Dimensions length/width/height [mm] | 247/300/249 |
| Density [kg/m3] | 800 – 850 |
| Weight [kg/pc] | Max. 15,7 |
| Compressive strength | P10/P15 |
| Masonry thickness [mm] | 300 |
| Consumption [pcs/m2] | 16 |
| Weight of masonry including plaster [kg/m2] | 280 |
| Fire resistance | REI 180 DP1 |
| Rw [dB] | 46 |
| Ru [m2K/W] | 1,73 |
| λu [W/mK] | 0,19 |
| Uext [W/m2K] | 0,50 |

(Source: http://www.wienerberger.cz/porotherm-30-profi-dryfix.html?lpi=1119439164442)

Porotherm 30 Profi Dryfix

Dimensions: Full brick, half-brick, corner brick

Bond of the walls at the corner